Splicing for Continuous Kicker

To join 2 pieces of rope (continuous kicker), you must first learn how to taper 4mm or 5mm Dyneema. It is important to use a high quality Dyneema and we would recommend that you use Marlow Excel Racing.

The inner core needs to be picked out of the outer core 30cm from the end of the rope. To do this bend the rope over at 30cm and use the fid to prise the outer core open and pick out the inner core. This may take some time and be careful not to damage the rope.

Once the inner core has been picked out, the outer core needs to be trimmed and fed back inside the inner core. Cut back the outer core, leave about 5cm and use a small amount of sellotape at the end of the outer core. This stops the outer core fraying and showing through the inner core.

Using the fid, the outer core can now be fed inside the inner core. This is done by feeding the fid down the centre of the inner core about 100mm, starting about 5mm from where the inner core comes out of the outer core. Then place the outer core into the fid and pull through.

Remove the fid, the outer core should be poking out of the inner core. Pull the outer core tight then slide the inner core up so the outer core slides inside.

A locking hitch will be required to secure to splice.

For a kicker you will need to do this twice, at each end of the rope. It may take sometime to work out the correct length. The tapers will need to overlap.

Two join the 2 ends together, lay the 2 taper ends next to each other, mark the middle of the tapers. Using the fid, feed one of the ends (end A) up the middle of end B, starting at the mark on end B, working towards the taper. Feed end A through until the two marks line up.

Remove the fid. The do the same with end B, feed the end up the middle of end A, starting 5mm for where end A entered end B.

Pull end B tight and remove fid.

Locking hitches will be required.